## Slide 1: Adhesives and fasteners

## Slide 2: Notes on adhesives
The “best” when they work correctly; “worst” when they fail
Determine the right adhesive for the job
Prepare adhesive and surface correctly
Use correct bond thickness
Fish line (monofilament) for spacers
Let cure before applying load; be patient!
Watch shelf life, mark date on new adhesive
Store in refrigerator or cool spot
Watch that maker has not “upgraded” adhesive
May no longer work like it used to
Prepare a properly engineered bonding procedure and use it!

## Slide 3: Bond line thickness

## Slide 4: Epoxy
Epoxy resin (uncured) is mildly toxic; wear gloves when using
Forms very strong bond, but is hard and somewhat brittle
Strong enough to pull apart glass; exercise caution
Two part adhesive; usually mixed 1:1, but not always
Cure rates/pot life variable with type and quantity of hardener
Fairly viscous but wets surfaces well and will flow
Clamp surfaces until at least partially cured
Debonds with heat but may have to get quite hot
Uncured resin cleans up with acetone

## Slide 5: Urethane
Has some give; it is a soft but tough adhesive
Maybe a substitute for RTV; similar properties
Two part adhesive with relatively short pot life
Very sticky; can get everywhere if not careful
Wets surfaces well; will bond plastics that others won’t
Uncured cleans up with acetone

## Slide 6: Bond thicknesses
For bonding metal to glass use a soft adhesive
One with give like RTV or urethane
Leave a thick bond line if possible
Can then cut off with thin wire if need to debond
Thick bond will be weak in shear
For low expansion, stable joints use very thin bond line
Adhesives have 10x or more CTE than glass/metals
Hard adhesive & thin bond, something will shear if two halves of bond expand at different rates
Note: epoxy cures exothermically, bond will get hot
Microspheres in cement for thin spacers

## Slide 7: Cementing optics like doublets
Use UV curing optical cement
Use 1 drop in concave element
Large lenses a challenge
Set mating surface on cement
Use orbital motion to work cement out to edge
Work slowly to avoid trapping air bubbles
Take apart if bubbles in joint
Center in “V” block or rotary table
Tack with UV light gun for 15-30 seconds
Finish cure with heat or soft UV lamp
Debond in boiling water or oil if water doesn’t work
Be patient, it may take hours

## Slide 8: Cementing tips
When potting optical elements in a cell, leave gaps in the cement, even a soft cement. Without gaps there is no place for the cement to expand or contract so the cement will act as though it were hard and distort the optics
Most adhesives shrink on curing. In most cases this is good, but beware, can cause distortion if surfaces not flat

## Slide 9: Debonding tricks
Always use eye protection; debonding unpredictable
Use CTE to your advantage; hot or cold so surface pulls away
Use shear by applying mechanical force via wooden clamp
Stress half of joint, then add shock
Usually hard cement will shear
If you plan to have to debond leave channels in the cement
so solvents, etc., can get to the interior of the cement

## Slide 10
http://www.tpub.com/content/bridges/TM-5-5420-278-24P/css/TM-5-5420-278-24P_385.htm
Reference for torques for screws. Go to “next” to find tables
http://www.gluguru.com/Adhesives%20Menu.htm
Reference for many types of adhesives

## Slide 11: Puck Bonding

## Slide 12: Puck Bonding
Primer
Actual puck
V-block
Bubble level
Reference circle
= 2.25arcmin

## Slide 13: Puck Bonding
Bonded puck
SMR nest with M6 thread for
puck position check

## Slide 14
Chart: Axial Puck Position - Bottom View Note Vertex Mark
Vertex Mark | 0
Zone A
Zone B
Zone C
UA wants to get approval from ATST

## Slide 15: Puck positioning
Laser
Tracker
SMR and Surrogate puck

## Slide 16: Surface Preparation
Surface prepared and protected
Surrogate puck
V-block
Kepton tape

## Slide 17: Puck Bonding Prep.

## Slide 18: Puck Bonding

## Slide 19: Quality Assurance
Puck Position and Tilt

## Slide 20: Quality Assurance

## Slide 21: Quality Assurance
Proof load test at 120% of normal loading

## Slide 22: Long Term Creep Test

## Slide 23: Typical failure mode
Cohesion vs Adhesion

## Slide 24: Mirror Support System
Left: Bonding of pucks to the mirror backplate; note the squeeze-out bead of Q3-6093 RTV around the perimeter of each puck (white disks). Right: Pucks & mirror support loadspreader frames on the backplate of an 8.4m honeycomb mirror.

## Slide 25: Creep

## Slide 26: Test

## Slide 28: Creep behavior of RTV-566

## Slide 29: Secondary stage Model vs Experiment