Opto-Mechanical Image Quality Degradation of Single Point Diamond Turned Plastics

Victor Villavicencio

Introduction

Textbooks usually provide first order optical equations to determine image quality.  This paper complements those equations by using opto-mechanical formulas which also affect optical performance. This article discusses how to calculate optical scatter using the “optical roughness” (), tilts, and thermal effects.  A major section will be informing the reader on optical scatter limitations.  The equations will finally be applied to a diamond turned plastic singlet example.

Approximations to Image Quality

In a laboratory environment where high power microwave or laser sources are used, scatter calculations are used to determine irradiance.  Irradiance values are required to properly select protection requirements for personnel and equipment. Classes and professional textbooks provide equations to calculate forward scatter from a diffraction-limited optical or microwave forward scatter at approximately 2.  Sigma or is the root mean square (RMS) wavefront error. As shown in the figure below, the forward scatter assumes a diffraction limited system (Strehl Ratio > 0.8).  The Strehl ratio is defined for a uniform intensity light or microwave wave entering a circular aperture.

Figure 1:  Scatter for a Diffraction limited System.  OPTI521 Fall Class notes.

In many applications, such as a plastic opto-mechanical system operating over a wide temperature range, diffraction limited performance (Wrms < 0.07 wave(length)) is not achieved.  Thus, when exceeding this limit, (Wrms > 1 wave(length))  how far can the forward scatter approximation be extended?

Scatter  limitations and Measurement Instruments.

When the average lateral extension of the microroughness, becomes much larger than, approximation equations for total integrated (back)scatter TISb and total forward scatter TISf (for transparent materials) are provided as [1a, 1b]:

TISb()  = (s / ( (s + (r) = 1 – e –(4   (cos(i/)  (                        (1)

TISf =                                                                 (2)

where  is laser source wavelength in microns

n is the refractive index of the transparent or reflective material under test.

(i is the angle of incidence on sample

is the total effective rms surface roughness, in microns, over frequencies from 0 to 1/.

(s, (r is the scattered and  reflectance power.

S2(f)   is the 2 Dimensional surface power spectral density  PSD (um4). It is a unit of measure obtained from optical profilers instruments.

| As shown in Figure 2, the approximate TIS is good for σ < ~λ/25. That is, for )/ > 0.04, the approximation underestimates the exact exponential form TIS [1a]. Equations 1 and 2 are normalized to the specularly reflected beam (not the incident beam), so TIS can be greater than 1. This will be shown in the Plastic system example. Note scaling laws for wavelengths other than  are provided in references 1a and 1b. | Figure 2: Comparison of the exponentially exact and approximate forms of the TIS backscatter Equations [1a] |
| --- | --- |

The total effective rms roughness  is defined by [1a]

(3)

From the PSD, the rms can be calculated by integrating the PSD over the bandwidth and taking the square root.  If the measurement area is a gaussian beam with a 6 mm diameter, then spatial periods that are larger than 6 mm can not be measured.  In other words, periods smaller than the measurement aperture will be affected because of the finite size of the measurement window or laser probe.

Figure 3: Nomarski micrographs of different surface structures [2].

| As shown in Figure 3, the scatter approximations of an optic depends not only on the height of periodic defects, but also on the relative size of the defects. Figure 4 shows the different equipment used to measure PSDs. In Figure 4, horizontal bars give the spatial wavelength ranges and the parentheses give the range of roughness heights that can be measured. [2] | Figure 4: Instruments used to measure surface topography. |
| --- | --- |

Background on the PSD

The Power Spectral Density (PSD) is a function that describes the amount of error in a surface a particular spatial frequency.  As an example for those who are not familiar with Fourier transforms, consider a sheet of sand paper with sand grains that are 100 m wide.  We can represent the sandpaper as a sum of sine waves with differing periods and magnitudes.  The most dominant sine wave would be the one with a period that is roughly the size of the sand grain or 100 m.  The frequency of this sign wave is 1 divided by the period so the frequency peak would be f = 0.01 m-1.

The lower order frequencies for optical components are typically specified using Seidel Aberrations, Zernike polynomial or some other polynomial fitting. It is usually the size of the part that determines the cutoff for this region.

The high spatial frequency region is typically the region where surface roughness will cause scattering of the lightwave or microwave.  At 1.07 microns, high spatial frequencies are any spatial period less than 120 m. This gives a high frequency cutoff of about 120 λ.  However, different instruments make measurements encompassing different image sizes to obtain the complete S2(f) , or PSD plot.

| Figure 5 shows a measured PSD for a real surface that includes segments that have been measured with four different instruments. The overlap agreement is quite good, although the actual PSD values measured with the optical profiler/white light interferometer (WLI) and the AFM differ by over 100 times at the high spatial frequency end of the WLI curve. This curve emphasizes again why there is no one value of the rms roughness for a given surface. It depends on the bandlimited spatial wavelength (or spatial frequency) range of the particular instrument. | Figure 5: PSD for an electroplated gold sample obtained from measurements with a Talystep mechanical profiler, atomic force microscope (AFM), white light interferometer (WLI) and angle resolved scattering (ARS). [2] |
| --- | --- |

Regardless, the calculated scattered powers from equations 1 and 2 can be reabsorbed by optics and mounts causing thermal effects.

Single Point Diamond Turned (SPDT) Plastic Example

Scatter approximations and measurement tools were reviewed since high power microwave or lightwave scatter can create thermal effects. Combining scatter calculations and opto-mechanical calculation, irradiance values can be calculated to properly select laser goggle optical density and determine image quality degradation due to thermal effects.

In this example, the author is attempting to measure a close-to diffraction limited spot size of a Single Point Diamond Turned (SPDT) Plastic Singlet over a 40( C temperature range.  The goal is to measure the minimum spot size by a knife edge method, with the following parameters:

10 mm diameter, f = 25 mm plastic singlet, the F-number is 2.5,

monochromatic source at  = 1 micron, CW power = 100 Watt.

From an optical Profiler, it is provided that Sq  ~  ( = 1064 nm) = 5 nm.

1) Select either the Styron or Radel Plastic:  From Table 1 Styron is selected since it is cheaper to prototype.

| Properties | Radel | Styron | 3M 2216 | Aluminum - 6061 | Invar 36 |
| --- | --- | --- | --- | --- | --- |
| Operating Temp. Range, Celsius | < 180 | 82 | -55 to 150 | < 900 | < 900 |
| Transmission - micron | 0.4 thru 2.0 | 0.4 thru 2.0 | opaque |
| Density - gram/cm^3 | 1.2 | 1.05 | 1.33 | 2.68 | 8 |
| Thermal Expansion Coefficient  - 10^-6 K-1 | 50 | 60 | 134 | 24 | 1 |
| Thermal coefficient of refractive index dn/dT 10^-6 | -5 | -10 | NA |  |  |
| Refractive Index at 1 um | 1.65 | 1.53 |  |  |  |
| Poisson Ratio | ?? | 0.34 | 0.43 |  |  |
| Surface roughness nm rms (excluding Haze) | < 5 | ?? | ?? |  |  |
| Flexural Modulus 10^9 N/m^2 | 2.9 | 2.5 | 0.24 |  |  |
| Thermo-Optic Coefficient,  | -57.69 | -78.87 | NA |  |  |

Table 1 – Material Properties under consideration for Best Form Singlet.

2) Calculate diffraction limited depth of focus: +/- 2  (F-number^2) = +/- 13 microns

3) Design Best form singlet: using n = 1.53, the radius of curvatures for the singlet were found to be R = 15.58 and R2 = -162.3

4) Select Mounting Style [3]

a) Edge-mounted               b)  Surface-centered          c) Cell-mounted

Figure 6:Various Mounting Techniques [3]

5) Calculate Optical Adhesive Gap [4, 200].

The optimum adhesive thickness (gap) at room temperature is calculated to be hr = 0.7 mm. That is, the optimum spacing is  2* hr =  inner mount diameter - outer lens diameter.

6) Calculate Tilt [3]

Figure 7 Accounting for tilt of a edge mounted element [3]

Using a semidiameter (SD) of 5 mm, R = 162 mm and a gap of 0.7 mm , a tilt of 2 degrees was calculated.  This tilt value is used to determine effects on image quality using Zemax.

7) Calculate the change in focal length [5]

The focal length expands, due to the t = 40 C temperature rise, by

| f = -( + housing) f T Where  is the plastic thermo-optics coefficient ,  is the CTE, f is the focal length, and T is the temperature range. From Table 2, 27 microns exceeds the 13 microns and therefore is outside the diffraction limits (See Figure 2). Thus, the forward scatter calculation underestimates the scatter. Since the Wrms is > 0.04 . adding actual surface roughness will only further increase the  value. | Table 2 – Plastic Singlet Dimensional Changes due to 40 C temperature rise. |
| --- | --- |

8) Simulate Image Quality Degradation

Go to Zemax and apply elevated temperature values from Table 2 and the 2 degree tilt into the optical design software.  The results for the knife-edge method is shown below. The figure below shows the focused spot has shifted from the mechanical center axis by approximately 100 microns.

Figure 8 – Elevated Temperature effects of Styron Singlet with a 2 degree tilt.

The effects above do not include radial temperature gradients.

9) Radial Temperature Gradient effects on Optical Path Difference [6, 799]

When a lens in air is subject to a radial gradient in which the glass near the rim is warmer than near the axis by an amount T, the OPD is

OPD = (nplastic – 1) tc p T = 0.58 * 0.005 meter * 60 x 10^-6* 40 = 7.5 um   = 6 waves at 1 um

Conclusion is the lens should be at thermal equilibrium before making a knife edge measurement.

10) Calculate Straylight

Note: when Calculating Back Scatter, using isotropic materials, such as plastics, the use of a one dimensional instead of two dimensional PSD is acceptable.  As shown in Figure 3, Untreated SPDT creates a one dimensional PSD, and therefore, a PSD calculated radially may be used.

( Powerreflected )* Eq. 1 = (100 * 0.053) * (4 Pi 0.08)^2 =  5.35 Watts backwards scattered.

(Powertransmitted) * Eq. 2 = (100* .9) * (0.091) = 8.1 Watts forward scattered.

Calculations have been shown to underestimate scatter with diamond turned plastics. That is, as shown in Figure 2, for )/ > 0.1, the approximation severly underestimates the exponential form TIS. A rough equation is being developed for )/ > 0.1, but not readily available [7]. Regardless, the calculated scattered powers can be reabsorbed by optics and mounts causing thermal effects.

Final Remarks

A thorough lens design tolerancing can be done only after a opto-mechanical layout is established.  The knife edge method, centered on the mechanical axis, may not provide the correct spot size diameter since the spot could be off by 100 um.

To reduce this 100 um offset, a doublet design will reduce this angular deviation, which then requires first order element pointing stability calculations [8],  besides another iteration of using the opto-mechanical equations.

This paper has provided image quality effects due to tilt, scatter, and temperature effects.  Programs such as Zemax or TracePro offer built in opto-mechanical assumptions. Those assumptions can now be compared with the opto-mechanical equations provided and referenced.

References

[1a] Michael G. Dittman, K-correlation power spectral density & surface scatter model, Optical Systems Degradation, Contamination, and Stray Light: Effects, Measurements, and Control II, edited by O. Manuel Uy, Sharon A. Straka, John C. Fleming, Michael G. Dittman, SPIE Vol. 6291.

[1b] Michael G. Dittman, Frank Grochocki, Kathleen Youngworth, No such thing as σ – flowdown and measurement of surface roughness requirements, Optical Systems Degradation, Contamination, and Stray Light: Effects, Measurements, and Control II, edited by O. Manuel Uy, Sharon A. Straka, John C. Fleming, Michael G. Dittman,  SPIE Vol. 6291.

[2] Jean M. Bennett, Dos and Don'ts in Characterizing and Cleaning Optical Surfaces Optical Fabrication, Testing, and Metrology II, edited by Angela Duparré, Roland Geyl, Lingli Wang, SPIE Vol. 5965 ( 2005)

[3] Frank DeWitt IV, Georg Nadorff, Rigid Body Movements of Optical Elements due to Opto-Mechanical Factors Optical Modeling and Performance Predictions II, edited by Mark A. Kahan, SPIE Vol. 5867, (2005)

[4] Vukobratovich, Introduction of Opto-Mechanical Design

[5] J.H. Burge, Opti521 Classnotes, Fall, 2006, University of Arizona..

[6] Paul R.Yoder, Opto-Mechanical Systems Design, CRC Press, 2006.

[7] John C. Stover, Rough Surface Characterization and Comparison of Scatter Measurements and Models, Advanced Characterization Techniques for Optics, Semiconductors, and Nanotechnologies II, edited by Angela Duparré, Bhanwar Singh, Zu-Han Gu, SPIE Vol. 5878

[8] J. H. Burge, An easy way to relate optical element motion to system pointing stability, Current Developments in Lens Design and Optical Engineering VII, Pantazis Z. Mouroulis, Warren J. Smith, R. Barry Johnson, Editors, SPIE, 6288